INFORMATION ON DOCTORAL THESIS

1. Full name:	 Tran Quoc Tuan		2. Sex: Male

3. Date of birth: 12/11/1981		4. Place of birth: Song Ma – Son La

5. Admission decision number: No 1691/ QĐ-SDH signed on 07/5/2009 by President of Vietnam National University, Hanoi.

6. Changes in academic process: Non

7. Official thesis title: Synthesis and investigation of silver/gold nanoparticles and its application.

8. Major: Solid State Physics			9. Code: 62440701

10. Supervisors: 			Assoc. Prof. Dr. Nguyen Hoang Hai

Prof. Dr. Nguyen Hoang Luong

11. Summary of the new findings of the thesis

- Proposed an improved sonoelectrochemical method overcoming the limitations of traditional sonoelectrochemical methods: Simple, inexpensive, uses less-toxic chemicals and easy to scale up.

- Proposed a detailed mechanism to explain the formation and growth of nanoparticles synthesised by improved sonoelectrochemical method and use simulation to demonstrate the correctness of the mechanism.

- Using silver nanoparticles to kill E. coli bacteria and downy mildew desease of grapevines.

- Coating the silver nanoparticles onto the carrier materials such as activated carbon and medical cotton gauze. Testing bactericidal effect of the carrier materials and use activated carbon impregnated silver nanoparticles to fabricate masks.

- Contents of the thesis were published in 5 articles including one belonging to SCI category (Q1) and 1 patent.

12. Paratical applicability, if any:

- The experiment results showed that silver nanoparticles have high applicability.

13. Further research directions, if any

14. Thesis-related publications:

[1] Tran Quoc Tuan, Nguyen Van Son, Hoang Thi Kim Dung, Nguyen Hoang Luong, Bui Thu Thuy, Nguyen Thi Van Anh, Nguyen Dinh Hoa, Nguyen Hoang Hai (2011), "Preparation and properties of silver nanoparticles loaded in activated carbon for biological and environmental applications", Journal of Hazardous Materials, 192, pp.1321–1329.

[2] Nguyễn Hoàng Hải, Nguyễn Đăng Phú, Trần Quốc Tuấn, Nguyễn Hoàng Lương (2013), "Synthesis of nanoparticles by chemical methods with the support of the physical impact", Journal of Science and Technology Development, pp.86-91.

[3] Trần Quốc Tuấn, Nguyễn Hoàng Hải, Dương Ngọc Tú, Đỗ Trung Thu (2013), "Application of Silver Nanoparticles for the Control of downy mildew desease on vines", 8th Nationally Proceedings Conference of Solid Physics and Materials Science (SPMS-2013), pp.402-405.

[4] Tran Quoc Tuan, Pham Van Hao, Luu Manh Quynh, Nguyen Hoang Luong, Nguyen Hoang Hai (2015), "Preparation and properties of silver nanoparticles by heat - combined electrochemical method", VNU Journal of science, 31 (2), pp.36-44.

[5] Trần Quốc Tuấn, Đỗ Đoàn Phúc, Nguyễn Hoàng Hải, Nguyễn Hoàng Lương, Nguyễn Thế Toàn (2013), "The mechanism of formation and development of silver nanoparticles prepared by sonoelectrochemical method", 9th Nationally Proceedings Conference of Solid Physics and Materials Science (SPMS-2015), pp.687-690.

[6] Nguyễn Hoàng Hải, Huỳnh Đăng Chính, Nguyễn Hoàng Lương, Trần Quốc Tuấn, Lưu Mạnh Quỳnh, Nguyễn Ngọc Long, Nguyễn Duy Thiện (2012), "Patent for Utility Solutions No. 963: Preparing the metal nanoparticles by sonoelectrochemical method", Department of Intellectual Property of Vietnam.